# Text boxes

•	Compressor oil: 9L01-0044 – PAO (polyalphaolefin) base synthetic hydrocarbon

compressor lubricant. The factory fills with Mobil Rarus SHC 1025, ISO Grade

46. Supported by Global Mobil Oil distribution network.

Substitutes must meet following ASTM standards below:

Viscosity, ASTM D445;				     	    SHC 1025

cSt @ 40°C     							44

cSt @ 100°C   							7.2

Viscosity Index, ASTM D2270, min    				131

Copper Strip Corrosion, ASTM D130,24h@100°C   		2A

Rust Characteristics Proc A, ASTM D665 				Pass

Flash Point, °C, ASTM D92						246

•	Engine oil: 9L01-0039 – API classification #CI-4, MIL SpecMIL-PRF-2104G, SAE

viscosity grade 15W40.

Factory Fill: Mobil Delvac Super 15W-40.

Meets requirements of all three current engine suppliers.

Supported by Global Mobil Oil distribution network.

SERVICE BULLETIN

SCHRAMM OIL SPECIFICATIONS – 2020

Note: This bulletin reflects the factory fill lubricants. Refer to your truck or engine manual for special cold or hot weather recommendations.

SERVICE BULLETIN

•	Hydraulic oil: 9L01-0067 – ISO class 46 hydraulic oil. Mobil DTE 10 Excel 46 Recommended when ambient temperature ranges are 10° to 110° F.

Use Mobil DTE  10 Excel 68 when ambient temperature ranges are 25˚ to 131˚ F

Supported by Global Mobil Oil distribution network.

Substitutes must meet following ASTM standards below:

Viscosity, ASTM D445;				     Excel 46	    Excel 68

cSt @ 40°C     						45.6		68.4

cSt @ 100°C   						8.45		11.17

Viscosity Index, ASTM D2270, min    			164		156

Copper Strip Corrosion, ASTM D130,3h@100°C   		1B		1B

Rust Characteristics Proc A, ASTM D665B 			Pass		Pass

Foam Sequence I, II, III, ASTM D892, ml			20/0		20/0

- Biodegradable Hydraulic oil: 9L01-0064 –  MOBIL EAL 224H, Mobil premium environmentally aware vegetable base HYD Fluid, Hydraulic systems operating with oil temperatures in the range of 0 F to 100˚F Substitutes must meet following ASTM standards below:

Viscosity, ASTM D445;				     EAL 224H

| cSt @ 40º C | 36.78 |
| --- | --- |
| cSt @ 100º C | 8.3 |
| Viscosity Index, ASTM D 2270 | 212 |
| Specific Gravity @ 15º C/15º C, ASTM D 1298 | 0.921 |
| FZG Gear Test, DIN 51354, Fail Stage | 12 |
| Vickers V-104C Pump Wear, ASTM D2882, mg | 10 |
| Aquatic Toxicity, LC50, Trout, OECD 203, ppm | ›5000 |

- Funk Drive Gearboxes (Pump Drive) 9L01-0049 – API GL-5 or SAE J2360.

Mobil  SHC150 Gear.

Supported by Global Mobil Oil distribution network.

Substitutes must meet following ASTM standards below:

Viscosity, ASTM D445;

cSt @ 40°C     						150

cSt @ 100°C   						22.2

Viscosity Index, ASTM D2270, min    			176

FZG Scuffing, ISO 14635-1 A/8.3/90 Fail Stage		13

•	Rotation Gearbox Synthetic Gear Lube: 9L01-0057 ISO grade 320.Must meet API service GL-5 or SAE J2360. If operating in sub- freezing conditions, it is recommended to use an ISO grade 220 synthetic gear lube.

Supported by Global Mobil Oil distribution network.

Substitutes must meet following ASTM standards below:

Viscosity, ASTM D445;				      SHC 220	       SCH320

cSt @ 40°C     						220		320

cSt @ 100°C   						30.4		40.6

Viscosity Index, ASTM D2270, min    			180		181

FZG Scuffing, ISO 14635-1 A/8.3/90 Fail Stage		14		14

FZG Scuffing, ISO 14635-1 A/16.6/90 Fail Stage		>14		>14

- Cable lubricant

VITALIFT 400: 9L01-0055 Cable Lubricant.

- Grease Specification- Lithium based

SERVICE BULLETIN